QUALITY CHECK PROCEDURE DURING APPLICATION

Procedure :  A patch of painted surface comprising base and top coat will be subjected to adhesion test in accordance with ASTM D3359 – cross hatch test. For this purpose, a cross will be made with a sharp tool/knife to reach the underlying metal surface. Next an adhesive tape will be affixed to cover the point of intersection and a small portion of the adjoining area and after a minute or so will be pulled off. No, to a very small portion (<5%), of the painted surface should be exposed to pass the test.  This test should be conducted 10 days after application of the top coat to permit ambient cure of the composite paint system. Suggested frequency of this test is once every 20 days during the course of bulk application.